## Slide 1: Y-Warm: Pioneer in Flexible Insulation Solution Beijing Matrix Technologies Co.,Ltd Jul. 2024
1
Website: http://www.y-warm.com
E-mail: fp.Zhong@y-warm.com

## Slide 2: Table of Content
Comparison of Y-Warm with a Renowned Brand
What is Y-Warm?
Application Fields of Y-Warm
How to Apply Y-Warm?
Supplementary Materials
Awards
Domestic and International Media Reports
Company introduction and history

## Slide 3: 1. Comparison of Y-Warm with a renowned brand
210g/㎡
53g/㎡
0
50
100
150
200
250
** B200
Y-Warm
Weight 4:1
4mm
0.9mm
0
1
2
3
4
** B200
Y-Warm
Thickness 4:1
$5.14/m
$2.5/m
0
10
20
30
40
** B200
Y-Warm
Cost 2:1
1.1 Comparison in Weight, Thickness and Cost
According to the evaluation provided by SATRA Technology Centre, comparisons of consumed weight, applied thickness and material cost between Y-Warm and a renowned material have been made to achieve the same insulation effect. More details please go to the supplementary page 17.

## Slide 4: 1.2 Comparison in Sustainability
4
Consumed/generated Applied material | Water (g) | Electricity (kW*h) | Petroleum (g) | CO2 (g)
Y-warm | 29.7 | 0.00297 | 3.3165 | 8.4645
Renowned brand | 118.2 | 0.01182 | 13.1990 | 33.6870
Reduction in value | 88.5 | 0.00885 | 9.8825 | 25.2225
Reduction in ratio | 75% | 75% | 75% | 75%
According to statics, the average consumption and exhaustion to produce 1 ton of raw fiber
material is listed as follows:
To produce a pair of shoes with a renowned brand, 39.4 g raw material is required. Whereas
9.9 g Y-Warm applied in the shoe can achieve an equivalent performance. 75% resource consumption can be saved and 75% CO2 will be avoided through the application of Y-Warm.
Water: 3 tons | Electricity: 300 kW*h
Petroleum: 0.335 ton | CO2: 0.855 ton

## Slide 5: 2. What is Y-Warm?
5
  Composition and Characteristics
    Envioronmental-friendly polymers with functional groups
    Polyester skeleton
Warm- keeping
Antistatic (half-life: 0.49 s)
Light and thin
Far- Infrared (Emissivity: 0.91 s Photothermaleffect:
2.8 °C)
ECO-
friendly
Moisture- permeable
Antibacterial (after 100 times of washing)
Quick- drying
Heat
Insulation
More information about insulation performance, permeability, antibacterial test, etc. can be found in the supplementary

## Slide 6: 2.2 Microstructure of Y-Warm
Cross-sectional Morphology of Y-Warm under SEM
Wall thickness: 20-280 nm
Pore size: 30-190 μm
Y-Warm internal structure: honeycomb

## Slide 7
3-D Pattern of Y-Warm under CT
Effective porosity is more than 96% (without skeleton).
White: wall of the bubble cell Black: hollow of the bubble cell

## Slide 8: 2.3 Value proposition of Y-Warm
Lowest density and lowest thermal conductivity among the existing textile functional materials.
Different from the fluffy insulation of down and synthetic fiber, Y-Warm offers a new concept of warm-keeping for winter fashion.
  Excellent tactile properties but light and non-fluffy.
  The tactility of Y-Warm stays stable and warm after storing at -60 °C for a week.
  Y-Warm can still float on water after soaked with water which several times of the original weight.
III.
Moisture-permeability and fast-drying.

## Slide 9: 2.4 Physical property of Y-Warm
Model code | Color | Thickness (mm) | Weight (g/m2) | Width (cm)
YW-01 | white/grey | 0.7±0.1 | 46±2 | 150±2
YW-03 | white/grey | 0.5±0.1 | 38±2 | 150±2
Model code | Color | Thickness (mm) | Weight (g/m2) | Width (cm)
YW-02 | white/grey | 0.9±0.1 | 53±2 | 150±2
YW-04 | white/grey | 1.0±0.1 | 70±2 | 150±2
Two series of material for Apparel
Two serials of material for footwear and hats

## Slide 10: 3. Application fields of Y-Warm

## Slide 11: 4. How to apply Y-Warm?
4.1 Application in Apparel
Filling sequence ：
fabric + Y-Warm + Lining
fabric + 1 layer of Y-Warm + fluffy material + Lining
fabric + 2 layers of Y-Warm + fluffy material + Lining
Please do
Diagonal cutting can maximize the elasticity.
Front and back sides functionalize equally.
Machine wash at room temperature.
Please DO NOT
High temperature and high pressure
Dense quilting

## Slide 12: 4.2 Application in Footwear
Please do
Apply in the middle layer
Sewing, or PUR hot melt adhesive lamination
Water wash at room temperature.
Please DO NOT
High temperature and high pressure
PUR hot melt adhesive is preferred avoid
destruction of the internal structure of the material
Full adhesive lamination affects moisture
permeability

## Slide 13: 5. Supplementary Materials
High water adsorption rate: 280% (twice as much as the standard fabrics tested).
Better drying rate: 60min (three times as much as the standard fabrics tested).
Excellent moisture-permeability allows the adsorption of the water vapor emitted from human body.
7.1 Moisture-permeability and Fast-drying of Y-Warm

## Slide 14: 5.2 Thermal Conductivity of Y-Warm Obtained from Different Test Methods
Test Method | Test Standard | Thermal Conductivity (W/m·K)
Sweating guarded-hot plate method | ISO 11092：2014.MOD | 0.00824
Guarded hot plate apparatus method | ISO 8302：1991.IDT | 0.026
Heat flow meter method | ISO 8301-1991 ASTM C518 | 0.0223
Transient plane source method Membrane module | Hot Disk-TPS3500 | 0.024
Transient plane source method Basic Module-One-sided | Hot Disk-TPS3500 | 0.016

## Slide 15: 5.3 Test report of Flex Resistance

## Slide 16: 5.4 Test report of SVHC

## Slide 17: 5.5 Test report of the comparison between Y-Warm and a renowned brand
Compared the performance of Y-Warm with a thickness of 0.9mm and well-known insulation materials with a thickness of 4mm,
and the test report from SATRA shows they can achieve the same warm keeping performance.

## Slide 18
5.6 To get more test reports, please visit our website:http://www.y-warm.com

## Slide 19: Technology tag
Clothing tag
Shoe tag
Sample package

## Slide 20: 6. Top Material Awards in 2020 and 2021
2020 ISPO Textrends Top 10
2021 ISPO Textrends Top 5

## Slide 21: 7. Domestic and International media reports
More than 600 media reports, including the Associated Press, Agence France-Presse, Bloomberg, European Post Gazette, Jiji Press, CCTV, etc..

## Slide 22: 8. Background of Y-Warm Technology And history
Since the discovery of nanoporous materials (e.g. Aerogel) in 1931, this material is considered as
a super insulator with the lowest thermal conductivity value of any known material.
Unfortunately, the application of Aerogel is strongly limited due to the difficulty to handle.
After eight years of exploration and efforts, Beijing Matrix Technologies Co.,Ltd has tackled the
world challenge on the combination of mechanical strength and thermal insulation.
The project of Y-Warm was launched in 2013. The technological breakthrough was achieved in
2017 and was panted in 2019. The mass production took place in the winter of 2021.

## Slide 23: 8.2 Beijing Matrix Technologies Co.,Ltd
Beijing Matrix Technologies Co.,Ltd has succeeded in developing of a new flexible insulation material Y- Warm and launched the mass production.
Address:
304, Block D, Zhongguancun ZhiZhuang Avenue, No.45 Chengfu Road, Haidian District, Beijing, PR China.
We provide a series of Y-Warm insulation material for different industrial applications. Currently we are not involved in other possible related business fields.

## Slide 24: The rules of 3R
International patented technology
A、Light and thin instead of heavy and thick;
B、Less mass material, higher insulation efficiency; C、Less carbon footprint, higher quality;
D、Less energy consumption, more environmentally friendly!
Reduce · Innovation achievement